## Slide 1
Introduction to Inelastic Neutron Scattering and handling powder INS data.
M. D. Le
India-RAL Neutron and Muon Science Meeting
Notes: The abstract pattern can be removed or repositioned if required. Be careful to ‘Send to Back’ so that it does not obscure any important information.

## Slide 2: Inelastic Neutron Scattering
Why?
Material properties depend on their structure
But, atoms are not stationary
Dynamics also important → inelastic neutron scattering can measure the dynamics of atom and spins.

## Slide 3
In elastic scattering, need to satisfy Bragg condition
Can be represented in an Ewald construction (sphere)
For inelastic scattering, |ki| ≠ |kf|
Now, have Q = ki – kf which defines the scattering triangle.
ki
kf
G
ki
Ewald’s sphere
ki
kf
G
ki
Q

## Slide 4: Single Crystals
The scattering triangle can be mapped directly to the axes of a 3-axis spectrometer
(ki and kf determined by Bragg diffraction from crystals)
ki
kf
ki
Q
ki
kf
q1
A4
q2
A3
A2
A1
A6
A5

## Slide 5: Single Crystals
The scattering triangle can be mapped directly to the axes of a 3-axis spectrometer
(ki and kf determined by Bragg diffraction from crystals)
ki
kf
ki
Q
ki
kf
q1
A4
q2
A3
A2
A1
A6
A5
Rotating crystal effectively rotates the scattering triangle.

## Slide 6: Powder samples
When we have a powder / polycrystalline sample, we have a random orientation of crystallites:
So the effectively we’re measuring an average over spherical shell of radius |Q|:
ki
kf
ki
Q

## Slide 7: Powder samples
When we have a powder / polycrystalline sample, we have a random orientation of crystallites:
So the effectively we’re measuring an average over spherical shell of radius |Q|:
ki
kf
ki
Q

## Slide 8: Powder samples
When we have a powder / polycrystalline sample, we have a random orientation of crystallites:
So the effectively we’re measuring an average over spherical shell of radius |Q|:
ki
kf
ki
Q

## Slide 9: Powder samples
When we have a powder / polycrystalline sample, we have a random orientation of crystallites:
So the effectively we’re measuring an average over spherical shell of radius |Q|:
ki
kf
ki
Q

## Slide 10: Triple Axis Spectrometers
Recap – for a TAS we can map the scattering triangle directly to the three axes of the spectrometer, where we control ki (or kf) by the scattering angles of the monochromator (analyser) crystals.
ki
kf
A4
q1
q2
A3
A2
A1
A6
A5
ki
kf
ki
Q
q1
q2

## Slide 11: Time-of-flight Spectrometers
At time-of-flight sources, only need to define one of ki or kf , the other is determined by the detector position and neutron time-of-flight.
There are two types of ToF spectrometers:
  “Direct geometry”: Fix ki
Direct geometry
kf
ki
Q
kf

## Slide 12: Time-of-flight Spectrometers
At time-of-flight sources, only need to define one of ki or kf , the other is determined by the detector position and neutron time-of-flight.
There are two types of ToF spectrometers:
  “Direct geometry”: Fix ki
  “Indirect geometry”: Fix kf
Indirect geometry
kf
ki
Q
ki

## Slide 13
Direct geometry spectrometers usually use mechanical choppers to monochromate the incident ki
Indirect geometry spectrometers usually use crystals to Bragg reflect a fixed final kf

## Slide 14: MARI
Spec
Ei = 7 meV to 1 eV
922 3He tubes; 3° to 130°
ΔE/Ei = 2.5 - 5%
Direct Geometry Instruments

## Slide 15: MAPS
Spec
Ei = 40 meV to 2 eV
40000 3He PSD elements; 3° to 20° - main bank 20° to 60° - high angle bank
ΔE/Ei = 1 - 5%
Direct Geometry Instruments

## Slide 16: MERLIN
Spec
Ei = 10 meV to 2 eV
π steradians of 3He PSDs
(gapless)
x20 Maps flux
x7 Maps detector coverage
ΔE/Ei = 4 - 6%
Direct Geometry Instruments

## Slide 17: LET
Spec
Ei = 0.5 meV to 20 meV
π steradians of 3He PSDs
(gapless)
Same flux/coverage as Merlin
ΔE/Ei = 0.6 - 3.5%
Direct Geometry Instruments

## Slide 18: Instrument suite
LET
MERLIN
MARI
MAPS
(Flux)
Ei (meV)
Q (Å)
Direct Geometry Instruments

## Slide 19: Around the world
Direct Geometry Instruments
ISIS | LET | MAPS | MERLIN
ILL | IN5 | - | IN4
SNS | CNCS | SEQUOIA | ARCS
J-Parc | Amateras | HRC | 4Seasons

## Slide 20: TOSCA
Indirect Geometry Instruments
n
Spec
Water moderator
E = 0~600 meV
ΔE/E = 1%
(energy transfer)
Detectors only around:
40-55° (forward)
125-140° (back)

## Slide 21: IRIS
Indirect Geometry Instruments
Spec
Hydrogen moderator
E < 4 meV
ΔE ~ 18µeV (PG)
High flux
Detectors 25<2θ<160°

## Slide 22: OSIRIS
Indirect Geometry Instruments
Spec
Hydrogen moderator
E < 4 meV
ΔE ~ 25µeV (PG)
Very high flux
Detectors 11<2θ<148°

## Slide 23: Around the world
Direct Geometry Instruments
ISIS | TOSCA | IRIS/OSIRIS
SNS | VISION | BASIS
J-Parc |  | DNA

## Slide 24
Questions so far?

## Slide 25: Phonons
Phonons are quantised lattice vibrations
Can be treated as collective motions of particles (mass m) connected by springs with force constant C
Simplest case of a monatomic chain:
With solutions:
Giving a dispersion relation:

## Slide 26
Phonons
0 0.2 0.4 0.6 0.8 1.0
q (π/a)
ħω
Transverse Acoustic Phonons
Longitudinal
Phonons
Phonons

## Slide 27
What does a INS phonon spectra look like?
See that there is much more intensity at high |Q| than low.

## Slide 28
The dynamical structure factor for phonon scattering is:
In a powder or polycrystalline sample, we have to average over all the directions of the momentum transfer Q.
At large |Q|>>|q| for a given |Q| the angular average is also approximately an average over a Brillouin zone so the term disappears and the term can be replaced by the density of states Z(E), giving:
This is called the incoherent approximation.
Phonon dynamic structure factor
Debye Waller factor
Polarization vector of mode d
Polarization factor
Methods of experimental physics: Neutron scattering Pt A by Sköld and Price, Ch 1

## Slide 29
Often though, the term is approximated as Q2, which is only correct if we average over a full Brillouin zone
But the take home message here is the neutron intensity of phonon scattering increases with increasing Q.

## Slide 30: Magnetic scattering
Due to the magnetic dipolar interaction between the neutron moment and electronic spins.
Scattering function for magnetic neutron scattering is:
Magnetic form factor is highest at low Q:
Because the electronic spins have a finite extent so their Fourier Transform is concentrated at low Q.
For phonons, scattering is due to the neutron-nucleus interaction, and nuclei are point particles compared to atoms
Magnetic excitations are most intense at low Q, opposite to phonon scattering.
Methods of experimental physics: Neutron scattering Pt A by Sköld and Price, Ch 1
M⊥ factor
Magnetic Form Factor

## Slide 31: Spin Waves
Quantised collective precession of spins – small deviations from ordered magnetic state
Dispersive, can look like phonons
But, most intense at low Q.
Unlike X-rays, magnetic intensity for neutrons can be larger than lattice vibrations.
Can be modelled using linear spin wave theory with SpinW in later part of course.

## Slide 32: Crystal Field
Transitions between localised electronic states with different Jz or Lz quantum number excited on a particular magnetic ion excited by neutrons.
Dispersionless, but follow form factor.

## Slide 33
Questions so far?

## Slide 34: Summary / Take home
INS can be visualised using the scattering triangle.
In continuous sources (reactors), need to define both the incident and scattered neutron energy / wavevector (ki and kf ).
In time-of-flight INS, only need to define either ki or kf and use the ToF to infer the other.
ToF where ki is fixed is direct geometry.
ToF where kf is fixed is indirect geometry.
There are different kinematic trajectories for each case.

## Slide 35: Summary / Take home
Phonons are quantised lattice vibrations (collective motions of atoms).
Phonon INS intensity is larger at high |Q| (approximately proportional to |Q|2).
Magnons are quantised spin precessions in an ordered magnetic state.
Crystal field excitations are excitations between localised electronic states with different with different Jz or Lz quantum number.
Magnetic excitations (magnons and crystal fields) follow the magnetic form factor and have highest INS intensity at low |Q|.

## Slide 36
@ISISNeutronMuon
isis.stfc.ac.uk
STFC
Notes: The abstract pattern can be removed or repositioned if required. Be careful to ‘Send to Back’ so that it does not obscure any important information.